Technical data Sheet

Foundry Green Moulding Process

Starch based additives

Complete range of starch and starch/bentonite blends ready to use, formulated to solve some typical problem in green moulding process :

- we can work with low bentonite  tax sands (4-5%) with consequent lower humidity and higher permeability; therefore casts with a better superficial aspect and minor tendency to pin-hole phenomenon;

- we can increase cohesion with the creation of a strong superficial crust in case; in this way we succeeded  in producing  even very big cast parts with the green moulding process

- we can work with high wet tensile strength  avoiding  a lot of superficial defects

- keep  an high level of sand

- no sand inclusions thanks to  deep painting  operations

The use of PRETAP, QUELL MELL and GELAMID increases considerably the sand plasticity and allows to  improve the accuracy of the dimensions and the cohesion, specially the edges. The PRETAP slows down the humidity’s evaporation and it avoids the formation of dust. This peculiarity simplifies the problems of hot moulding sand, and it reduces the arise of superficial imperfection

|  |  | Pretap | Quell mell | Gelamid | Gelamid 10 | Stahlsec |
| --- | --- | --- | --- | --- | --- | --- |
| Moisture Umidita’ Humidité | % | 12 max | 12 max | 12 max | 12 max | 12 max |
| pH | % | 6-7 | 8-9 | 8-9 | 8-9 | 13-18 |
| Ashes Ceneri Cendres | % | 0,35 | 65 max | 50 max | 80-85 | 70 -75 |
| Bulk density Peso specifico apparente Poid specifique theorique | kg/dm3 | 0,55 | 0,6-0,7 | 0,6-0,7 | 0,6-0,7 | 0,5-0,6 |
| First adds Aggiunte iniziali Premières ajoutes | % | 0,5-0,8 | 0,5-0,8 | 0,5-0,8 | 0,5-0,8 | 0,8 |

# Text boxes

foundry@laviosa.com

ADVANTAGES ON GREEN MOULDING HOT (1)

0

100

200

300

400

500

600

700

800

900

1000

1100

0

0,5

1

1,5

2

2,5

3

3,5

H

2

O

With additive

Without additive

GCS(g/cm2)

ADVANTAGES ON GREEN MOULDING HOT (2)

0

10

20

30

40

50

60

70

80

0,5

1

1,5

2

2,5

3

3,5

4

H

2

O

COMPATTABILITY' (%)

Without additive

With additive

.