Technical data sheet

Foundry Shell moulding process

Precoated sand LH

Laviosa Chimica Mineraria developed the production of its resin coated during the past 30 years, gaining a substantial knowledge technological characteristics the materials and the process we employ must have for ensuring a constant high quality output of the finished products. In particular we experienced that the chemical composition and the fines content of the sand , the shape and the size distribution of the grain, together with the quality of the resins, play a crucial role in the production of our resin coated sands. The constancy of the quality  is continuously monitored thought a fixed program of controls with comprises the following laboratory tests.

| Precoated sand | LH 25/70 | LH 35/70 | LH 50/70 | TH 70/90 |
| --- | --- | --- | --- | --- |
| GRAIN SIZE INDEX GRANULOMETRIA GRANULOMETRIE | [DIN] | 50/55 | 50/55 | 50/55 | 92/102 |
| THICKNESS AFTER 20” BAKING; 280° C SPESSORE DOPO COTTURA 280 ° C 20” EPEISSEUR APRES CUIVRE 280°C 20” | [mm] | 7,5/8,5 | 7,5/8,5 | 7,5/8,5 | 8,0/9,0 |
| BAKING RATE VELOCITA’ DI COTTURA VELOCITE’ CUIVRE | [sec] | 80/90 | 80/90 | 80/90 | 90/100 |
| LOSS OF IGNITION PERDITA CALCINAZIONE PERTE AU FEU | [%] | 3,0-3,4 | 3,5-3,9 | 3,9-4,3 | 4,5-5,0 |
| TENSILE STRENGHT RESISTENZA TRAZIONE RESISTENCE TRACTION | [kg/cm2] | >25 | >35 | >45 | >50 |
| TRANSVERSE STRENGTH RESISTENZA FLESSIONE RESISTENCE FLEXION | [kg/cm2] | >50 | >70 | >80 | >100 |

# Text boxes

foundry@laviosa.com