Technical data sheet

Foundry Green Moulding Process

PREMIX®

Coal/bentonite blend ready to use for green moulding process

Coal/bentonite ready to be used mix – called PREMIX - are fundamental in order to avoid the following problems: customer’s waste of time in mixing operations; Bentonite/Coal mistakes in the percentage; logistic difficulties in silos storage, phenomena of auto -combustion.  These mixtures can be produced with coal percentages / bentonite customer as by customer’s suggestions

| STANDARD PREMIX |  | Premix 25N/75B | Premix 30N/70B | Premix 35N/65B | Premix 40N/60B |
| --- | --- | --- | --- | --- | --- |
| Moisture Umidita’ (sul prodotto tal quale) Humidité | [%] | 9-12 | 9-12 | 9-12 | 9-12 |
| Volatile substances Sostanze volatili (base secca) Résidu volatil | [%] | 13-16 | 14,5-17,5 | 16-19 | 17,5-20,5 |
| Ashes Ceneri (base secca ) Cendres | [%] | 69-73 | 67-71 | 60,5-64,5 | 56,5-60,5 |
| Fixed carbon Carbonio fisso Carbone fix | [%] | 11-17 | 14-20 | 17-23 | 19-26 |
| Lustrous carbon Carbonio brillante (base secca ) Carbon brillant | [%] | 2-3 | 2,5-3,5 | 3-4 | 3,5-4,5 |
| Coesion Coesioni Coésion | sabbia LA 32 - compattabilità 65% - premix (su base 7% bentonite) |
| Green compr. Strenght Resistenza alla compr. Verde Resistence compression | [g/cm2] /cm2 | >1200 | >1200 | >1200 | >1200 |
| Wet Tensile Strenght Resistenza allo strato umido Resistence à Haute Humidité | [g/cm2] | >45 | >45 | >45 | >45 |
| STANDARD PREMIX |  | Premix 50N/50B | Premix 60N/40B | Premix 70N/30B | Premix 80N/20B |
| Moisture Umidita’ (sul prodotto tal quale) Humidité | [%] | 9-12 | 5-9 | 5-9 | 5-9 |
| Volatile substances Sostanze volatili (base secca ) Résidu volatil | [%] | 20,5-23,5 | 23,5-26,5 | 26,5- 29,5 | 29,5-32,5 |
| Ashes Ceneri ( base secca ) Cendres | [%] | 48-52 | 40-42 | 31-35 | 23-27 |
| Fixed carbon Carbonio fisso Carbone fix | [%] | 25-31 | 30-36 | 36-42 | 41-47 |
| Lustrous carbon Carbonio brillante ( base secca ) Carbon brillant | [%] | 4,5-5,5 | 5,5-6,5 | 6,5-7,5 | 7,5-8,5 |
| Coesion Coesioni Coésion | sabbia LA 32 - compattabilità 65% - premix (su base 7% bentonite) |
| Green compr. Strenght Resistenza alla compr. Verde Resistence compression | [g/cm2] /cm2 | >1200 | - | - | - |
| Wet Tensile Strenght Resistenza allo strato umido Resistence à Haute Humidité | [g/cm2] | >45 | - | - | - |
| LEGEND 1st numb.: % coal dust 2nd numb.: % of bentonite | LEGENDA 1^ cifra: % di nero utilizzato 2^ cifra: % di bentonite | LEGEND 1er num. :% de noir 2eme num.: % de bentonite |

# Text boxes

foundry@laviosa.com

.